## Slide 1
Formulation and Optimization of Ethosomes and Liposomes of Fluconazole for Transdermal Delivery
A
Thesis / Dissertation Submitted
to
Oriental University, Indore
for the award of the Degree of
Master / Doctor of Philosophy
in
Faculty of Pharmacy
Supervisor
Dr. ...........
Faculty of Pharmacy
Submitted by
Gulfisha
Enrollment No: ...............
ORIENTAL UNIVERSITY, INDORE

## Slide 2
AIM
Formulation, development and evaluation of ethosomes of fluconazole for transdermal delivery, with liposomes prepared as a comparator vesicular system.
Ethosomes & Liposomes of Fluconazole
2

## Slide 3
OBJECTIVES
To perform preformulation studies of fluconazole.
To formulate, characterize and optimize ethosomes of fluconazole using Design of Experiments (DoE).
To prepare and evaluate fluconazole liposomes as a comparator.
To compare drug release and stability of ethosomes and liposomes.
To perform antifungal activity of the optimized formulation.
Ethosomes & Liposomes of Fluconazole
3

## Slide 4
ABSTRACT
Fluconazole, a triazole antifungal, was formulated into ethosomal and liposomal gels to enhance transdermal delivery for topical antifungal therapy.Vesicular systems were prepared and optimized using a Taguchi screening design followed by response surface methodology (RSM), studying the effect of key variables on vesicle size and entrapment efficiency.Optimized batches were incorporated into Carbopol gels and evaluated for drug content, pH, spreadability, viscosity, in-vitro drug release, morphology (TEM), stability and antifungal activity against Aspergillus niger and Candida albicans.Ethosomal gels showed higher entrapment, enhanced and sustained drug release, and superior antifungal activity compared with liposomal and marketed formulations.
Ethosomes & Liposomes of Fluconazole
4

## Slide 5
Base Paper for Defending Title
Akhtar N. et al. (2012) — Cavamax W7 composite clotrimazole ethosomes developed using a 3² factorial design.
  Optimized composite formulation (F9): entrapment efficiency 98.42%, zeta potential −83.6 mV, vesicle size 202.8 nm.
  Cumulative in-vitro permeation reached 88.53% in 8 hours with higher antifungal efficacy against Aspergillus niger and Candida albicans.
  Establishes composite/optimized ethosomes as advanced antifungal vesicular systems — basis for applying DoE-optimized ethosomes to fluconazole.
Ethosomes & Liposomes of Fluconazole
5

## Slide 6
Literature Review
Sr. No. | Author/Authors, Year | Title / Focus | Source / Publisher | Findings & Relevance | Research Gap
1 | Zhao et al., 2014 | FLZ liposomal gel (film dispersion) | Research article | Oval/round vesicles, EE ~47.68%; superior drug retention in rat skin (depot effect) despite lower cumulative permeation. | Limited RSM optimization
2 | Majumdar et al., 2014 | FLZ liposomes in hydrogel | Research article | 2² factorial + RSM studying hydration volume and phospholipid:cholesterol ratio on EE and release. | No ethosome comparison
3 | Habib et al., 2008 | Ophthalmic FLZ liposomes (reverse-phase evaporation) | Research article | Negatively charged liposomes gave fastest corneal healing in Candida keratitis rabbit model vs. neutral/positive and FLZ solution. | Ocular, not topical skin
Ethosomes & Liposomes of Fluconazole
6

## Slide 7
Literature Review
Sr. No. | Author/Authors, Year | Title / Focus | Source / Publisher | Findings & Relevance | Research Gap
4 | Ola et al., 2010 | Multilamellar FLZ liposomes (thin-film hydration) | Research article | α-tocopherol acetate greatly increased EE; membrane composition strongly affects physicochemical performance and stability. | No gel / antifungal test
5 | Bhalariya et al., 2009 | FLZ ethosomes vs. liposomes (clinical) | Clinical study | Ethosomes (hot method) vs. liposomes (film hydration); ethosomal formulations showed greater clinical efficacy in candidiasis. | FLZ + RSM gel lacking
6 | Akhtar et al., 2012 | Clotrimazole composite ethosomes (3² factorial) | Research article | F9: EE 98.42%, zeta −83.6 mV, size 202.8 nm; 88.53% permeation in 8 h; active vs. A. niger & C. albicans. | Different drug (clotrimazole)
Ethosomes & Liposomes of Fluconazole
7

## Slide 8
Literature Review
Sr. No. | Author/Authors, Year | Title / Focus | Source / Publisher | Findings & Relevance | Research Gap
7 | Sarat et al., 2011 | Ketoconazole ethosomes (modified hot process) | Research article | Ethosomal cream delivered drug across membrane far more effectively than conventional non-ethosomal cream. | Different drug (ketoconazole)
8 | Touitou et al., 2000 | Ethosomes - novel vesicular carriers | J. Control. Release | Introduced ethosomes; high ethanol content enables deep skin penetration and enhanced transdermal delivery. | General, not FLZ-specific
Ethosomes & Liposomes of Fluconazole
8

## Slide 9
Research Gap
Limited response surface methodology (RSM)-based optimization for fluconazole vesicular systems.
No direct quantitative comparison of ethosomal and liposomal fluconazole under identical experimental conditions.
Few gel-based ethosomal topical systems with dedicated antifungal efficacy testing for fluconazole.
Need for systematic in-vitro permeation and stability comparison of the two carriers.
Ethosomes & Liposomes of Fluconazole
9

## Slide 10
RESEARCH METHODOLOGY
Vesicular systems (ethosomes & liposomes) of fluconazole prepared and optimized using Design of Experiments.
  Screening of influential variables using Taguchi design.
  Optimization of vesicle size and entrapment efficiency via response surface methodology and intensive grid search.
  Optimized vesicles incorporated into Carbopol gels.
  Gels evaluated for physicochemical properties, in-vitro release, stability and antifungal activity.
Ethosomes & Liposomes of Fluconazole
10

## Slide 11
PLAN OF WORK / FLOWCHART
Exhaustive literature search
Preformulation study of fluconazole (organoleptic, calibration curve, solubility, partition coefficient, LOD, pH, melting point, flow properties)
Drug-excipient compatibility (FTIR & DSC)
Preparation of ethosomes & liposomes using DoE factorial design
Characterization: particle size & entrapment efficiency; variable screening + grid search
Preparation & characterization of fluconazole gel
In-vitro skin permeation, stability study and antifungal activity vs. marketed gel
Ethosomes & Liposomes of Fluconazole
11

## Slide 12
RESEARCH WORK
Materials
  Fluconazole (API), lecithin / soya phosphatidylcholine, cholesterol, ethanol, Carbopol, buffers.
Preparation of ethosomes
  Phospholipid + drug dissolved in ethanol; aqueous phase added under stirring (cold/hot method).
Preparation of liposomes
  Lipid film hydration using lecithin and cholesterol; hydrated and size-reduced.
Taguchi screening design used to identify critical variables for both systems.
Ethosomes & Liposomes of Fluconazole
12

## Slide 13
RESEARCH WORK
Preformulation studies of fluconazole
  Organoleptic properties and physical appearance
  Calibration curve (UV) in ethanol and phosphate buffer pH 7.4
  FTIR and DSC for identity and melting point
  pH, flow properties (angle of repose, Carr’s index, Hausner ratio)
  Solubility, partition coefficient, loss on drying
  Drug-excipient compatibility by FTIR & DSC
Ethosomes & Liposomes of Fluconazole
13

## Slide 14
RESEARCH WORK
Evaluation of vesicles and gels
  Vesicles: entrapment efficiency, vesicle/particle size, morphology (TEM)
  Gels: drug content, pH, spreadability, viscosity
  In-vitro drug release via Franz diffusion cell
  Release kinetics: zero-order, first-order, Korsmeyer-Peppas models
  Stability: effect of storage temperature on vesicle size and drug content
  Antifungal activity vs. Aspergillus niger and Candida albicans
Ethosomes & Liposomes of Fluconazole
14

## Slide 15
RESULT & DISCUSSION
Fluconazole identity confirmed (FTIR, DSC); linear UV calibration; no significant drug-excipient incompatibility.
Taguchi screening + RSM identified critical variables; grid search located optimum ethosome and liposome compositions.
Ethosomes achieved higher entrapment efficiency than liposomes.
Ethosomal gels showed enhanced, sustained in-vitro release (Korsmeyer-Peppas / diffusion-controlled).
TEM confirmed spherical vesicles; refrigerated storage preserved size and drug content best.
Ethosomal gel showed superior antifungal activity vs. liposomal and marketed gels.
Ethosomes & Liposomes of Fluconazole
15

## Slide 16
CONCLUSION
Fluconazole ethosomes and liposomes were successfully formulated and optimized using DoE.
Ethosomes provided higher entrapment and enhanced, sustained drug release.
Ethosomal gel demonstrated superior skin permeation and antifungal activity.
Ethosomes are a promising carrier for transdermal antifungal delivery of fluconazole.
Ethosomes & Liposomes of Fluconazole
16

## Slide 17
FUTURE SCOPE
Ex vivo and in vivo studies in animal models to confirm efficacy and safety.
Scale-up and long-term ICH stability studies of the optimized formulation.
Explore combination antifungal therapy and other poorly permeable drugs.
Investigate clinical translation of ethosomal topical systems.
Ethosomes & Liposomes of Fluconazole
17

## Slide 18
REFERENCES
Zhao et al., 2014. Fluconazole liposomal gel for topical antifungal delivery.
Majumdar et al., 2014. Optimization of fluconazole liposomal hydrogel.
Habib et al., 2008. Ophthalmic fluconazole liposomes.
Ola et al., 2010. Multilamellar fluconazole liposomes.
Bhalariya et al., 2009. Fluconazole ethosomes vs. liposomes (clinical).
Akhtar et al., 2012. Clotrimazole composite ethosomes.
Touitou et al., 2000. Ethosomes - novel vesicular carriers, J. Control. Release.
Ethosomes & Liposomes of Fluconazole
18

## Slide 19
LIST OF PUBLICATIONS
1. ...........................................................................2. ...........................................................................3. ...........................................................................
Ethosomes & Liposomes of Fluconazole
19

## Slide 20
THANK YOU
20